## Slide 1
Presented by
Ed Matthiesen
Biochar and Iron Sand Media

## Slide 2: E. COLI TMDL LOAD REDUCTION
Shingle Creek TMDL Load Reduction Curve

## Slide 3: IN SUMMARY
Need big reductions in nutrients, sediment, and bacteria
No handy point sources – diffuse non-point sources
Fully developed, highly impervious
Few opportunities for significant new structural BMPs

## Slide 4: BIOCHAR BACKGROUND
Research by Dr. Sanjay Mohanty, UCLA
Column study showed biochar could remove up to 99% E. coli from stormwater, compared to 62% with just sand
SK Mohanty, AB Boehm. 2014. Escherichia coli removal in biochar-augmented biofilter: Effect of infiltration rate, initial bacterial concentration, biochar particle size, and presence of compost.
Environmental Science & Technology. 48 (19), 11535-11542.

## Slide 5: IRON/SAND BIOCHAR MEDIA
Iron/sand 5% by weight purchased premixed from Plaisted Companies.
Biochar produced by Char Energy, LLC. Made from hard wood at 500°C. Optimally installed at 30% by volume.

## Slide 6
Coon Creek Watershed Biochar
“Agricultural Carbon” by National Carbon Technologies
Source Material: Wood burned >550C
Surface area: 339 m2/g
Composition:
      84% Fixed Carbon
      12% Volatile matter
      4% Ash
99.95% E. coli removal in lab trial
Valenca et al. in prep
Notes: Countless varieties of biochar depending on source material, pyrolysis temperature, post-processing… no standard exists… hard time choosing, so we sent 4 commercially available biochars to UCLA for testing to find out which worked best for e coli capture specifically.
158 cy biochar which equates to over 1650 sq miles surface area… the northern half of the 7 county metro
UCLA results: removal capacity positively correlated with surface area and carbon content, negatively correlated with ash content and % volatile organic matter

## Slide 7: CATCH BASIN INSERTS TP REMOVALS

## Slide 8: CATCH BASIN INSERTS E. COLI REMOVALS

## Slide 9: Minnesota Filter
Graphic: Andy Erickson, SAFL
Now with biochar!

## Slide 10: CHAMPLIN POND IN OPERATION

## Slide 11: CHAMPLIN TP REMOVAL

## Slide 12: CHAMPLIN E. COLI REMOVAL

## Slide 13: POND 2: CRYSTAL NORTH LIONS PARK IRON/SAND ONLY

## Slide 14: CRYSTAL E. COLI REMOVAL (NO BIOCHAR, IRON/SAND ONLY)

## Slide 15: Biochar- & Iron-Enhanced Sand Filters
Woodcrest Creek
Treats 1 sq. mi. area
2 cfs gravity system
75% TP/82% E.Coli removals (preliminary)
Football field, in scale
Pleasure Creek
120-200 gpm pumped system
Treats 200-300 af/yr
26-43 lbs TP/yr

## Slide 18: CONTACT INFORMATION
Ed Matthiesen, P.E.
ed.matthiesen@stantec.com
763-252-6851