## Slide 1: Bioretention media
Mike Isensee, CPESC
Middle St. Croix Watershed Management Organization Washington Conservation District
Mike Isensee, CPESC Middle St. Croix WMO
Washington Conservation District

## Slide 3: Infiltration –Use Compost

## Slide 4
Filtration with Most Infiltration Credit (per MIDS Calculator)

## Slide 6
Compost
P
P
P
P
P
P
P
P
P
P
P
P
P
P
P
Bannerman 2013
Engineered Media

## Slide 7
1.Ensure Media Mixture to a P content between 12-30 mg/kg (and supports vegetation).
2. Incorporate a soil amendment to facilitate absorption of P (and does not kill vegetation).
Engineered Media

## Slide 9
 | Mix A: Water quality blend | Mix B: Enhanced filtration blend | Mix C: NC State water quality blend | Mix D | Mix E: MnDOT 3877.2 Type G 'Filter Topsoil Borrow' | Mix F: Custom Infiltration Basin Planting Soil
Fine aggregate for Portland Cement Concrete |  |  |  |  | 60-80% | 
Construction Sand | 55-65% | 50-70% |  |  |  | 
Sand |  |  | 85-88% | 60-75% |  | 
Loamy Sand |  |  |  |  |  | 75%
Topsoil | 10-20% |  |  |  |  | 
Silt and Clay |  |  | 8-12% |  |  | 
Organic Matter | 25-35% | 30-50% | 3-5% |  |  | 
MnDOT grade 2 compost |  |  |  | 20-40% | 20-40% | 25%
MN Stormwater Manual Mixes
Growing media must be suitable for supporting vigorous growth of selected plant species.
The pH range (soil/water 1:1) is 6.0 to 8.5
Soluble salts (soil/water 1:2) should not to exceed 500 parts per million
All bioretention growing media must have a field tested infiltration rate between 1 and 8 inches per hour.

## Slide 10
Required Testing
Soil media test results and a soil sample must be submitted at least 14 days prior to material delivery.
Analysis | ($) | Standard Turnaround Time | Sample Amount Needed
9045 pH Soil | 21 | 4 Hours | 50 grams
ASTM D2974 Organic Matter | 42 | 2 Days | 50 grams
Phosphorous (Bray) | 75 | 2 Days | 60 grams
365.1 Total Phosphorous | 32 | 2 Days | 20 grams
CEC | 93 | 3 Days | 200 grams
Grain Size | 177 | 5 Days | 200 grams

## Slide 11
Date | Media | Olsen P | Bray P | Melich3
 |  | ppm | ppm | ppm
9/1/2015 | 60/40 Sand/Peat | 22 | 26 | 
9/15/2015 | 60/40 Sand/Peat |  | 10 | 
6/9/2015 | 70/30 Sand/Sphag. Peat |  |  | 6
6/1/2015 | 80/20 Sand/Sphag. Peat |  |  | 12
6/1/2015 | 70/30 Sand/Sphag. Peat |  |  | 6
6/1/2015 | 80/20 Sand/Compost |  |  | 68
6/1/2015 | 70/30 Sand/Compost |  |  | 114
4/1/2014 | 70/30 Sand/Compost |  | 66 | 
4/1/2014 | 70/30 Sand/Reed Sedge Peat |  | 12 | 
4/1/2014 | 70/30 Sand/Sphag. Peat |  | 11 | 
7/1/2013 | 60/40 Sand/Sphag. Peat |  |  | 10

## Slide 12
Current Standard
70/30 Sand/Sphagnum Peat
Test Results Required

## Slide 13
1.Ensure Media Mixture to a P content between 12-30 mg/kg (and supports vegetation).
2. Incorporate a soil amendment to facilitate absorption of P (and does not kill vegetation).

## Slide 14
95% ASTM C-33 Coarse Wash Sand and 5% Iron Aggregate by weight (1,485 lbs. Connelly GPM Inc., ETI CC 1004 or approved equal).
Iron Enhanced Sand

## Slide 15
IESF is Exposed to the Air
Extra Underdrain (w/ gate valve)
Key Design Considerations

## Slide 16: Key Design Considerations
Iron Sand Filter
High Flow Bypass
Maximize filtration prior to discharge to the IESF

## Slide 17
5% Iron filings (dry weight)?
Oven Dry
1,000 Gram Media Sample (approximately 2 cups)
Separate the sample with a magnet
Weigh abstracted Iron
Repeat
Quality Control
Iron
Sand & Iron
Magnet & Iron
Iron

## Slide 18
Erickson, A.J., J.S. Gulliver, and P.T. Weiss. 2007. "Enhanced sand filtration for storm water phosphorus removal, Journal of Environmental Engineering." 133 (5): 485-497.
Erickson, A.J., J.S. Gulliver, and P. T. Weiss. 2012. “Capturing Phosphates with Iron Enhanced Sand Filtration,” Water Research, 46(9), 3032–3042.

## Slide 19
Weiss, P., Aljobeh, Z., Bradford, C., and Breitzke, E. (2016) An Iron-Enhanced Rain Garden for Dissolved Phosphorus Removal. World Environmental and Water Resources Congress 2016: pp. 185-194. doi: 10.1061/9780784479889.020

## Slide 22: Targeting Stormwater Pollutants
Settling
Physical
Biological Filtration Bacterial Degr.
Chemical
Sorption
Sump Forebay
Pond
Weeper
Weir
Skimmer
Reactive Sand Filter
Bioretention Cell
Infiltration

## Slide 23: Lake St. Croix 2017
12.75 Acres Total Watershed
1,440 cubic feet IESF
Binding capacity 40 lbs.
Total Annual Load = 12.46 lbs. P
Annual Dissolved P Reduction = 2.1 lbs. P
City of Stillwater 2017 Eng. Estimate $96,000

## Slide 24
Engineered Media

## Slide 25
Thank You!
Curt Coudron, CPESC, Senior Resource Conservationist
Jim Davidson, CPSWQ, CPESC, Urban Conservationist
Media Mixes & testing standards
Mike Isensee, CPESC Watershed Specialist misensee@mnwcd.org
New Bioretention
Bryan Pynn, Senior Water Restoration Technician
Questions?
Mike Isensee, CPESC Administrator MSCWMO misensee@mnwcd.org
Andy Erickson, Researcher, St. Anthony Falls Laboratory, University of Minnesota